## Slide 1
The Van der Waals and Electrostatic Interaction
Studying of
Crystalline Cellulose Iβ Based on Molecular Dynamics
——Xue-Wei Jiang, Hong-Hui Zhang, An-Hua Zhong

## Slide 2
01.Background
1
03.Results and discussions
04.Forecast
02.Methodology and Processing
Materials
Cellulose fibers are
important mature of textile
and other materials
Interactions
Hydrogen bonding is the main
binding forces between chains,
it is not all for stacking sheet
Molecular dynamics
Molecular dynamics approach is
an effective computer modeling
technology
Cellulose Iβ

## Slide 3
Building the initial structure
with cellulose-builder
All simulation were performed with
Amber software and explicit water
Calculate the interaction energy by program
MMPBSA.py of AmberTools
02.Methodology and Processing
2
03.Results and discussions
04.Forecast
01.Background

## Slide 4
02.Methodology and Processing
3
03.Results and discussions
04.Forecast
01.Background
a = 7.784 Å,b = 8.201 Å,
c = 10.38 Å
α = β = 90°,γ = 96.5°
c is the chain direction
About the initial modeling

## Slide 5
02.Methodology and Processing
4
03.Results and discussions
04.Forecast
01.Background
Step.01
Step.03
Step.02
Step.04
Set the initial environment
Various temperatures:298K,350K,
400K,450K,500K,550K
Force field:GLYCAM-06
Set the periodic
boundary condition
A 12Å buffer of TIP3P water around
the cellulose Iβ in each direction
The two stages of
minimization procedure
Firstly the water was minimized.
Then the whole system.
Run molecular
dynamics
Firstly heat the system with restraints.
Then run MD Equilibration
The simulation processing with software Amber

## Slide 6
At 298 K, the Van der Waals and
electrostatic intermolecular energy per chain are -43.91 kcal/mol and -26.24 kcal/mol respectively. The Van der Waals energy gradually reduces when the temperature rises, meanwhile
the electrostatic energy increases initially and then decreases.
03.Results and discussions
5
01.Background
04.Forecast
02.Methodology and Processing

## Slide 7
The electrostatic energy of most glucose residues for intrachain lies on 11-14 kcal/mol and 5-8 kcal/mol, while located on 7-10 kcal/mol and 2-5 kcal/mol at 298 K for interchain. The Van der Waals interaction energy in intrachain increases slightly as the temperature rises and there is almost no growth for interchain.
03.Results and discussions
6
01.Background
04.Forecast
02.Methodology and Processing

## Slide 8
The intersheet Van der Waals interaction decreases slightly with the temperature increasing, The Van der Waals energy of most glucose residues is located on the range of 6-12 kcal/mol at 550 K.
03.Results and discussions
7
01.Background
04.Forecast
02.Methodology and Processing

## Slide 9
The interactions were discussed only in water, and no comparison to other solvents. In the next step, we will study the Van der Waals and electrostatic interaction in different solvent environments.
04.Forecast
8
03.Results and discussions
01.Background
02.Methodology and Processing

## Slide 10
THANK YOU .
Notes: 模板来自于 http://docer.wps.cn